PRODUCT SPECIFICATION – QuietZone Acoustic Batt Insulation

Section 09 80 00 Acoustical Treatment

Section 09 85 00 Sound transmission Control Materials

Part 1 – GENERAL

  - Summary

- Glass fiber acoustical insulation for interior walls, floors and ceilings in residential, multi-family

and commercial buildings.

  - Related Products

- Section 09 85 00 -QuietZone Acoustic Sealant

- Section 09 85 00 -QuietZone Acoustic Floormat

- Section 09 85 00 -QuietZone Acoustic Wall Framing

- Section 09 77 40 -QuietZone Solserene Fabric Ceiling System

- Section 09 54 00 –QuietZone Acoustyle Wood Ceiling System

  - References

- American Society for Testing and Materials (ASTM)

  - E84 Test Method for Surface Burning Characteristics

  - E90 Laboratory Measurement of Airborne Sound Transmission Loss  of Building Partitions and Elements

  - E96 Test Method for Water Vapor Transmission of Materials

  - E136 Test Method for Behavior of Materials in a Vertical Tube Furnace at

750 degrees F. (unfaced)

  - C423 Test Method for Sound Absorption and the Sound Absorption Coefficient

by the Reverberation Room Method

  - C665 Standard Specification for Mineral Fiber Blanket Insulation for Light Frame

Construction and Manufactured Housing.

  - Submittals

- Product Data:  Submit Owens Corning product literature, installation instructions and product

samples for specified insulation.

  - Delivery, Storage and Handling

- Protect insulation from physical damage and from becoming wet, soiled or covered with ice or snow.

Comply with manufacturer’s recommendations for handling, storage and protection during installation

- Label for insulation packages to include material name, production date and/or product code.

  - Limitations

- Do not use unfaced insulation in exposed applications where there is potential for skin contact

and irritation.

- Kraft facings will burn and must not be left exposed.  The facing must be in substantial contact

with the unexposed surface of the ceiling, wall or floor finish.

Part 2 – PRODUCTS

2.01 Manufacturer

A.  Owens Corning

2.02 QuietZone Acoustic Batt Insulation

A.  Type I: Unfaced glass fiber insulation complying with ASTM C 665 and ASTM E 136.

B.  Type II: Kraft faced glass fiber insulation complying with ASTM C 665.

C.  Surface burning characteristics

1.  Unfaced Insulation

Maximum flame spread: 10

Maximum smoke developed; 10

2.  Kraft faced Insulation

Maximum flame spread:  not rated

3.  Maximum smoke developed:  not rated

D.  Combustion Characteristics:  Unfaced insulation passes ASTM E 136 test.

E.  Dimensional Stability:  Linear stability less than 0.1%.

Part 3 – EXECUTION

3.01 Inspection

A.  Examine the areas and conditions under which work of this section will be installed.

Verify that adjacent materials are dry and ready.  Verify that electrical and

mechanical sevices within walls have been inspected and tested.  Verify that project

drawings comply with installation requirements.

B.  Provide written report listing conditions detrimental to the performance of work in

this section.  Do not proceed with installation until unsatisfactory conditions have

been resolved.

3.02 Installation

A.  Comply with manufacturer’s instruction for particular conditions of installation

in each case.

B.  Between wood studs

Friction-fit unfaced insulation between studs after cover material has been installed

on one side of the cavity.  When faced insulation is used, staple attachment flanges

to face or side (preferred) of stud every 8 to 12 inches to hold in place.

3.03 Installation – Vapor retarder

This insulation is for interior wall use only.

The Kraft paper for this product is NOT a vapor retarder.

NOT recommended for exterior walls.

3.04 Material Storage and Protection

Protect insulation from damage and from becoming wet before, during and after installation.

END OF SECTION